CERTIFICATE OF ANALYSIS

Date:			November 5, 2007

Material:		Aluminum Metal Powder, spherical

Lot No.:		ACN2060B

CAS #:			7429-90-5

Customer:		Sung-Bo Corp

Ra-1308 Zoongang Youtong Danzi

Goorobondong 1258, Goorogoo Seoul Korea

Purchase Order No.:	71031

Chemical Analysis:  (%)

Iron		  <0.011

Aluminum	>99.989

Screen Analysis

FSSS:    	2.9 microns

Average particle size: 	1-3 microns

The above analysis is carried out as part of our internal quality control testing and is based upon our analysis methods.

We do not assume any warranty, liability or risk based on such findings.  Our quality is warranted within the scope of our general sales conditions.

Brenda Lyons

Managing Member